## Slide 1
Engineering Macromolecular Hydrophobicity to Induce Phase Separation and Microstructure in Biomaterials
Ellen Blackwell, Saniya Yesmin Bubli, Matthew Smolag, Linqing Li*
Department of Chemical Engineering, University of New Hampshire, Durham, NH 03824, USA
* Linqing.Li@unh.edu
Changing overall hydrophobicity of the macromolecule.
Higher molecular weight exhibits lower transition temperature.
Reversible phase transition demonstrates true LCST behavior.
Introduction
NH BioMade IIA 1757371 and EPS-1101245
CIBBR (P20GM113131) at NIH
UNH Core facility and Instrumentation Center
Engineered macromolecular hydrophobicity in dextran induces phase separation and microstructures for biomedical applications.
Phase separated hydrogel with defined microstructures regulate cellular behavior.
Future plans include characterizing mechanical properties of hydrogels and designing a two-component system for stabilization.
1. H. K. Lau, L. Li, A. K. Jurusik, C. R. Sabanayagam, and K. L. Kiick, “Aqueous Liquid-Liquid Phase Separation of Resilin-Like Polypeptide/Polyethylene Glycol Solutions for the Formation of Microstructured Hydrogels,” ACS Biomaterials Science and Engineering, 3, 757–766, 2017.
2. C. G. Garcia and K. L. Kiick, “Methods for producing microstructured hydrogels for targeted applications in biology _ Enhanced Reader,” Acta Biomaterialia, 84, 34–48, 2019.
3. A. C. Daly, L. Riley, T. Segura, and J. A. Burdick, “Hydrogel microparticles for biomedical applications,” Nature Reviews Materials, 5, 20–43, 2020.
Compositional heterogeneity and microstructural properties are essential in regulating cellular behavior1.
Phase separation is a single step procedure to control microstructure in biomaterials2.
Application of photo-crosslinking to capture microstructures in biomaterials to enhance cell-matrix interaction.
These novel phase-separated hydrogels with defined microstructures can be used towards tissue vascularization and wound healing.
Phase contrast and fluorescent images of human dermal fibroblasts cultured on hydrogels without phase separation (top) and with phase separation (bottom).
Reversible LCST Behavior of Thermoresponsive Dex-MA
Phase-Separated Hydrogels Regulate Cell Adhesion
Addition of Surfactants Inhibiting Phase Separation
Hydrophobic Adducts to Induce Phase Transition
Quantification of Microparticles via SEM​
References
LCST phase separation of dextran-MA with different degree of methacrylation
Phase separation
SEM image of Dex-MA microparticles before and after phase separation
Acknowledgement
Turbidity assay of Dex-MA
Effects of denaturing agents (SDS and Urea) on LCST
Cationic salts
Cationic salts have a minimal effect on LCST.
Anionic salts have a greater effect on LCST.
Systematically increase the functionality of methacrylate to regulate LCST.
Lower percentages exhibit a higher LCST and a faster reverse transition.
Increased concentration exhibits lower LCST.
Comparison of data obtained from DLS and UV-Vis.
Tuning of LCST using Hofmeister Salts
Tunable Parameters to Modulate Phase Separation
Conclusions
Addition of strong surfactant sodium dodecyl sulfide (SDS) eliminates phase separation.
Addition of mild surfactant (urea) gradually shifts the LCST.
Confirms the hypothesis that association of phase separation is mediated by hydrophobic interaction.
Dex-MA above LCST (45oC)
Dex-MA below LCST (22oC)
Temperature induces LCST
Tuning LCST via degree of methacrylation
No phase separation
Reversible profile of dextran
MW and methacrylation dependent LCST
Concentration profile with transition temperature
Hydrogel microparticles for endogenous tissue repair3
Microstructured hydrogels formed from RLP/PEG that undergoes phase separation1
Synthesis of dextran methacrylate (R=H/methacrylate)
Schematic of reversible phase transition via modifying dextran backbone with methacrylate
Dextran is an uncharged hydrophilic homopolysaccharide and FDA approved material.
Chemical routes to introduce hydrophobic residues (methacrylate) onto hydrophilic dextran backbone to induce LCST.
Multi-parameters for tuning transition temperature.
Anionic salts
Microparticle size distribution
UNH ChE Department
Dr. Linqing Li’s Lab, UNH
Dr. Jeffrey Halpern’s Lab, UNH
Dr. John Tsavalas’s Lab, UNH
Dr. Nate Oldenhuis’s lab, UNH
DAPI/Phalloidin/ Vinculin