## Slide 1
Enhancement of Plasmonic Gold Catalysts for Photocatalytic Methane Conversion
Samuel Mercer and Dr. Nan Yi
Department of Chemical Engineering, University of New Hampshire, Durham, NH 03824
Introduction
Localized Surface Plasmon Resonance (LSPR)
Machine Learning for Catalyst Design
Material Characterization and Tuning LSPR
Acknowledgments
Significance and Conclusions
References
Methane is a potent greenhouse gas that is the main component of natural gas, providing energy worldwide. Although it is an important fuel for combustion, it also holds promising potential to be reutilized for direct conversion to desirable chemicals (such as methanol and syngas).
Methane has a high thermodynamic barrier that requires high activation energies of 435 kJ mol-1.
Photocatalytic reactions may facilitate methane conversion through a novel nanocomposite design, Au-HPA-TiO2, that absorbs light to generate free radicals (rather than by traditional thermal or electrochemical methods).
Clean usage of methane for chemical production is possible with photocatalytic methane conversion at ambient conditions.
The composition of the photocatalyst heavily influences its plasmonic resonance. The powerful computational model programmed provides data that analyzes, models, assesses, and filters the most viable catalyst designs for methane conversion.
Future research may improve the application of computational methods and further characterize the photocatalyst. The synergistic effect of a bimetallic photocatalyst may also be investigated.
//
Chart: Wavelength [nm]
Effect of HPA structure
[1] Horn, Raimund and Schlögl, Robert. Catal. Lett. 145: 23-29, 2015.
[2] Kozhevnikov, Ivan. Chem. Rev. 98: 171-198, 1998.
[3] Zakaria, Zulfirdau and Kamarudin, Siti Kartom. Renew. Sust. Energy. Rev. 65: 250-261, 2016.
[4] Toyao, Takashi et. al. ACS Catal. 10(3): 2260-2297, 2020.
[5] Song, Hui et. al. Joule 3(7): 1606-1636, 2019.
//
//
Catalyst Synthesis and Activity Testing
Metal-NP | Polyoxometalate (HPA) | Method
Au (0.5 wt%) | H3PW12O40 (5 wt%) | Deposition-Precipitation
Au (0.5 wt%) | H3PW12O40 (12 wt%) | Deposition-Precipitation
Au (0.5 wt%) | H3PW12O40 (15 wt%) | Deposition-Precipitation
Au (0.5 wt%) | H3PW12O40 (20 wt%) | Deposition-Precipitation
Au (1 wt%) | H4PW12O40 (20 wt%) | Deposition-Precipitation
Au (1 wt%) | H3PW12O40 (12 wt%) | Deposition-Precipitation
Au (0.5 wt%) | N/A | Impregnation
N/A | H3PW12O40 (20 wt%) | Impregnation
N/A | H4PW12O40 (20 wt%) | Impregnation
Ir (0.3 wt%) | H3PW12O40 (15 wt%) | Deposition-Precipitation
Methodology
//
Electric field enhancement
Probabilistic Modeling of Methane Adsorption
Calculation of Electronic Properties using DFT
//d
//d
//d
//
Deposition-precipitation method
Photocatalytic activity testing
CH4 (10%)
Ar (90%)
(2.5%)
(2.5%)
(5%)
Ar (90%)
H2O2 (5 mL)
hv
//
Chart: Wavelength [nm]
Effect of Au loading
//
Chart: Wavelength [nm]
//
Chart: Wavelength [nm]
Effect of HPA loading
Different nanocomposite designs
Combined experimental and computational approach.
Assisted learning neural networks are trained to predict plasmon resonance based on catalyst properties surveyed in literature and experimentally.
Supervised learning for synthesis parameters
ML predicted LSPR band gap reaction coordinate
The activity and selectivity of the optimal catalyst design for methane conversion is modeled using kinetic Monte Carlo (kMC) simulations from an open-source Python-based interface.
Electronic properties and material behavior were calculated based on density functional theory by programming a simplified lattice model in C++ for the optimal photocatalyst from QuantumESPRESSO.
Lattice model and potential energy surface
Elevated loading of Au nanoparticles negates plasmonic activity while increased HPA loading enhances it. However, HPA addition also hinders catalyst stability and leads to sintering at lower temperatures.
Thermogravimetric analysis confirmed that all variants of the Au-HPA-TiO2 synthesized decomposed at elevated temperatures and lost stability.
Ir-HPA-TiO2 showcased heightened levels of stability at elevated temperatures, demonstrating that metallic alloys have unique synergistic properties with HPA.
Experimental results are combined with those from literature to create a library of catalyst designs. This database of catalyst syntheses provided valuable data to quantify the optimal synthesis parameters and tune the material design.
Thank you to Dr. Nan Yi, Dr. Gonghu Li, Dr. Gagandeeph Singh, Dr. Guoqiang Cao, Ehab Shaaban, and Darcy Fournier for supporting my research.
UNH Hamel Center for Undergraduate Research
UNH University Instrumentation Center, Department of Chemical Engineering, and Department of Chemistry
Au-H3PW12O40 (HPA)-TiO2
//d
Kinetic Monte Carlo reactivity model
Simulated elementary steps
Novel catalysts are designed to enhance activity, selectivity, and stability for photocatalytic methane conversion.
Data is queried into a library for ML-assisted analysis and ab initio simulations prior to lab experimentation.
//
Illustration of LSPR mechanism
Chart: Wavelength [nm]
Ten photocatalysts were synthesized with unique loadings.
Activity testing was accomplished by preparing a packed bed photoreactor loaded with 5 mL of H2O2 for steady state methane flow under 300W UV light.
LSPR is an effect of incident light on the gold nanoparticle that causes conduction band electrons to oscillate, enhancing the electric field on the particle’s surface and prompting radical formation at photocatalyst active sites.
Low yield of desirable products prompted mechanistic study of LSPR effects on Au-HPA-TiO2 photocatalysts.