## Slide 1
Electrochemical Characterization of the Stimuli-Response of Surface-Immobilized Elastin-like Polymers
Marissa A. Morales1, Eva Rose M. Balog2, Jeffrey M. Halpern1
Contact: mm1452@wildcats.unh.edu or jeffery.halpern@unh.edu
1Chemical Engineering, University of New Hampshire 2Chemistry and Physics, University of New England
SURFACE-IMMOBILIZATION
STIMULI-RESPONSE
ELECTROCHEMICAL IMPEDANCE SPECTROSCOPY
Tt influenced by ELPs structure or solvent conditions
  Decreases Tt – ELPs experience isothermal stimuli-response
Transition Temperature (Tt):
T < Tt - ELPs are solvated with decreased intermolecular interactions
T > Tt - Decreased solubility with increased intermolecular and intramolecular interactions
STIMULI-RESPONSE
ELASTIN-LIKE POLYMERS
X = Isoleucine (I)
n = 40 pentapeptide repeats
Alternating Voltage Potential
Redox Couple
Ferri/Ferrocyanide
Extended
Collapsed
Rct(Extended) < Rct(Collapsed)
Rct
Z – Real (Ohms)
-Z – Imaginary (Ohms)
Nyquist
Randles Circuit
0.0125 mg/mL I40
3.5 mM TCEP pH 7
T = 4˚C
t = 0.5 hours
ACKNOWLEDGEMENTS
Surface-immobilization of I40 was dependent on the thiol interaction with gold and reproducible
ELPs are intrinsically disordered, adopting environment dependent conformations
(Val-Pro-Gly-X-Gly)n
ELPs share a repetitive pentapeptide sequence
The authors would like to acknowledge the University of New Hampshire Graduate School, Pilot Research Project of the Collaborative Research Excellence Initiative at University of New Hampshire, NSF EAGER CBET 1638896 (JMH), NSF EAGER CBET 1638893 (ERMB), and NSF MRI 1531296 for the funding of this work.
Extended
Collapsed
0.0 M NaCl
3.0 M NaCl
0.5 M NaCl
0.75 M NaCl
Collapsed
Extended
1.0 M NaCl
T < Tt
T > Tt
I40
(Val-Pro-Gly-Ile-Gly)40
I40-Blocked: Contains cysteine residue modified using iodoacetamide
Electrochemical impedance spectroscopy was used to characterize the stimuli-response of surface-immobilized I40 demonstrating reversibility and intermediate stimuli-responses
Extended
0.0 M NaCl
Collapsed
3.0 M NaCl
Iodoacetamide
ΔRct = Rct(3.0 M NaCl) – Rct(0.0 M NaCl)
ΔRct(I40) = 16,400 Ω
ΔRct(I40-Blocked) = 84 Ω
Notes: Template File: 1901_CIBBR Retreat_MAM