## Slide 1
Ice formation is a global issue that poses serious challenges for many applications.
AF(G)P’s have a complicated structure:
Modifications of this PVA and
similar polymers have been
reported, yet many fundamental
relationships between structure
and performance remain.
Synthesis and characterization of Trehalose g lycopolymers and studying the OH orientation role in INI, IRI, and THA.
Sorbitol conjugation to the polymer to improve INI at lower concentration and its impact on IRI and THA.
Studying ice nucleation rate impact on IRI activity of AFPs and antifreeze polymers.
Introduction
Next Steps
References
This research is supported by NASA research group .
University of New Hampshire, Chemistry department.
NASA group for funding and collaboration.
Acknowledgements
Figure 12. General schematic representation of a 3D porous network manufactured from the directed assembly of pre-structured microparticles.
Thermal hysteresis Activity (THA)
Modification and Characterization of Polyol Based Polymers for Ice Recrystallization Inhibition and Thermal Hysteresis Activity
Mohammad Mousazadehkasina, John Tsavalasa, Paul Bauresb, Krisztina Vargac, Emily Asenath-Smithd
Ice recrystallization inhibition (IRI)
Ice Nucleation Inhibition (INI)
Polymer Synthesis and Characterization
mPIP
mPMAA
mPAA
807.4 (µm2 )
mPVA
95 (µm2 )
7302.4 (µm2 )
5980 (µm2 )
6856.5 (µm2 )
7309 (µm2 )
PBS
Polymer | THA
mPAA | 0.47±0.03
mPMAA | 0
mPVA | 0.64±0.09
PVA | 0.24±0.07
mPIP | 0
AFP | 0.59±0.03
ΔT = TNs (Polymer solution ice nucleation point) – (-17.7) (PBS ice nucleation point)
Polymer impact on heterogenous Ice nucleation inhibition (INI):
-20 °C
0 °C
-38 °C
Homogeneous ice nucleation
Heterogenous ice nucleation
Differential scanning calorimetry (DSC) has been used to study heterogenous ice nucleation for polymer solution.
Hydroxyl groups concentration on mPVA is higher than PVA which same distance (2.7 Ao)and it leads to more effective interaction with growing crystals. Another factor is the flexibility of the mainchain in mPVA and PVA. We speculate intramolecular interaction in mPAA and mPMAA diminish IRI activity.
100-500 nm
10-30 µm
IRI activity was evaluated by monitoring the growth of polynucleated ice crystals using splat assay at subzero temperatures, to allow
recrystallization eﬀects to be separated from nucleation.
From the data, mPVA and PVA have effective interaction with water molecules in metastable phase which disturb water molecules and leads delay in nucleation2. mPMAA and mPIPA promote heterogeneous ice nucleation by increasing total surface area for nucleation.
PVA, Poly(isopropanol) (PIPA), poly(acrylic acid) (PAA), and poly(methacrylic acid) (PMAA) used as starting polymers to graft a series of pendent functional structures. FTIR and 1H NMR used for characterization and confirmation .
The difference between melting and nonequilibrium freezing temperatures of ice in an aqueous solution defined as thermal hysteresis and is used as a characteristic measure for antifreeze activity 5, 6, 7. DSC used for measuring THA of modified polymers.
1. Hakim, Aaron, et al. "Crystal structure of an insect antifreeze protein and its implications for ice binding." Journal of biological chemistry 288.17 (2013): 12295-12304.
2-Baruch, E.; Mastai, Y., Antifreeze Properties of Polyglycidol Block Copolymers. 2007, 28 (23), 2256-2261.
3-Mochizuki, K.; Qiu, Y.; Molinero, V., Promotion of homogeneous ice nucleation by soluble molecules. Journal of the American Chemical Society 2017, 139 (47), 17003-17006.
4.Li, L.-f.; Liang, X.-x., Influence of Adsorption Orientation on the Statistical Mechanics Model of Type I Antifreeze Protein: The Thermal Hysteresis Temperature. The Journal of Physical Chemistry B 2017, 121 (41), 9513-9517.
5.Li, L.-f.; Liang, X.-x., Influence of Adsorption Orientation on the Statistical Mechanics Model of Type I Antifreeze Protein: The Thermal Hysteresis Temperature. The Journal of Physical Chemistry B 2017, 121 (41), 9513-9517.
6.Ding, X.; Zhang, H.; Wang, L.; Qian, H.; Qi, X.; Xiao, J., Effect of barley antifreeze protein on thermal properties and water state of dough during freezing and freeze-thaw cycles. Food Hydrocolloids 2015, 47, 32-40.
7. Stubbs, Christopher, et al. "Multivalent Presentation of Ice Recrystallization Inhibiting Polymers on Nanoparticles Retains Activity." Langmuir (2018).
2.92 oA
(RiAFP. Beta-Strands1 )
(PVA interaction with prism plane of ice)
Industry
Food science
Cell/Organ preservation
THA = Th – To
Experimental XRD patterns