## Slide 1
Novel 3D Printing Process for Improved Mechanical Properties of Tissue Engineering Scaffolds Jackie Desrosiers, Kyung-Jae Jeong*
Department of Chemical Engineering, University of New Hampshire, Durham, NH 03824
*Corresponding Author KyungJae.Jeong@unh.edu
Schematic
Introduction
Methods
Live/Dead Confocal Imaging
Acknowledgements
Research Summary
Biocompatibility of 3D Printed Structure
A 3D printed bio-ink provide​s a complex structure with precise placement of cells and ECM, in a layer-by-layer process
Potential Applications
Modeling for disease and tissue development
Methods to repair, regenerate, or replace damaged tissue
Challenges
Biocompatibility of the bio-ink and crosslinking methods
Mechanical stability of the crosslinked hydrogel
Goals
To print a biocompatible ink with improved mechanical properties (stiffness and strength)
For the bio-ink to show noticeable advantages over current methods and solutions
Crosslinking Methods
Photo-polymerization (GelMA)
Ionic crosslinking (Alginate with Ca2+)
Enzymatic crosslinking (Gelatin and mTG)
Preparation of Bio-ink
Sterile solution of Irgacure (0.5% w/v), Gelatin (5% w/v), and GelMA (5% w/v)
Autoclaved alginate (1% w/v) added and dissolved at 37 ℃
Rheological Testing
TA Instrument AR 550
Viscosity measured as a function of shear rate
Stiffness measured as a function of time and angular frequency
Cell Culture
HDF cultured at 37 ℃ and 5% CO2
DMEM media supplemented with 1% penicillin/streptomycin and 10% bovine serum
HDF concentration of 5 x 106 cells/mL mixed in bioink
3D Bioprinting
BioAssemblyBot 400 & TSIM modeling software
Bioink printed at 27 ℃, 10-15 psi, and 5 mm/s
Analysis
Live/Dead Confocal Imaging
AlamarBlue Assay
LDH Assay
This research was sponsored by the U.S. National Science Foundation and was accomplished under the Grant No. OIA-1757371. Thank you to Mrinal Ganash for all his help and Maria Skidmore and Patrick Earley for their previous work.
Bio-ink proved to be a shear-thinning fluid
Addition of both mTG and calcium crosslinking greatly increased the hydrogel stiffness
Live/Dead assay showed biocompatibility of the bio-ink and 3D bioprinting method
Over 7 days, HDF cells spread and proliferated with minimal cell death
Delayed crosslinking of calcium showed slightly better cell proliferation than immediate calcium crosslinking
Physical Characterization of Bio-Ink
Day 1
Day 7
Prepare bio-ink and cell mixture
UV + mTG + Ca2+
UV + mTG + Ca2+ (delayed)
UV Only
Print 3D Scaffold
Crosslink via UV light
Crosslink via mTG and Ca2+ bath
AlamarBlue Assay Results, measuring cell proliferation over time
LDH Assay Results, measuring cytotoxicity through cell plasma membrane damage within the sample
a) Viscosity measurement of bio-ink solution at varying temperatures
b) Storage modulus of hydrogel as it crosslinks overtime
a)
b)
c)
d)
c) Bio-ink stiffness measurement of different crosslinking methods
d) Bio-ink strength measurement of different crosslinking methods
UV + mTG
Day 7 – 3D Projection
GelMA crosslinked via UV radiation
Alginate crosslinked via Ca2+
Gelatin crosslinked via mTG