## Slide 1
Novel Plasmid DNA Macrocyclic Bottlebrush Polymer
Synthesis
Introduction
Motivation. Advances have been made toward generating bottlebrush polymers with unique topologies and assemblies, but synthetic methods and dispersity limitations remain. In this work, biologically derived linear pUC19 plasmid DNA (pDNA) serves as a backbone for synthetically made poly(ethylene glycol) methyl ether mustargen (mPEG-CEA) to alkylate under biologically relevant conditions. By varying the molecular weight mPEG-CEA and the concentration relative to the pDNA, a variety of macrocyclic bottlebrush polymers can be generated with this method. Visualization of the formed bottlebrushes was achieved through the combination of atomic force microscopy (AFM) and agarose gel electrophoresis. This method serves as a facile route to achieve PEGylated DNA materials which can significantly improve DNA’s ability to be used as a material in the future.
Modified PEG side chains
Conclusions & Future Work
References
Acknowledgements
Preliminary Results. Using agarose gel analysis, the pDNA displayed differences in size by changing the molecular weight of PEG-mustargen (Mw 2000 vs 750). The highest Pegylated pUC19 PEG-mustargen2000 appeared at ~4500 bp while PEG-mustargen750 showed at ~3500 bp
Conclusion
Future Work
Gel Electrophoresis
Figure D. Reaction scheme for synthesis of mPEG-bis-chloroethylamine. All structures were confirmed using 1H NMR. n = 750, 2000, 20000
Figure E. Proposed mechanism for alkylation of DNA with via intramolecular cyclization (aziridinium formation) of the mustargen followed by nucleophilic attack by the N7 position of guanodine
Figure A. Reaction scheme for synthesis of pDNA bottlebrush polymer and structure of side chains of the bottlebrush polymer
Acknowledgements – This research was supported with funding from the National Science Foundation’s Research Experience for Teachers in Engineering Grant (ENG-1132648).
This research is supported by a National Science Foundation EPSCoR award (#1757371).
Rationale Design of pDNA Bottlebrush. Mustargen compounds are well known compounds capable of alkylating DNA allowing for straightforward grafting-to handles1. PEG is a well established, FDA approved polymer with known compatibility for conjugation to DNA and other biomolecules in part due to properties such as high-water solubility2. The chosen linearized plasmid, pUC19 was derived from a high plasmid yielding fed-batch fermentation process developed by the Oldenhuis lab. This allows for a polymer backbone of a known size which can be characterized using well established techniques like agarose gels and AFM.
Sauter, B.; Gillingham, D. DNA Damaging Agents in Chemical Biology and Cancer. CHIMIA 2020, 74 (9), 693.
Alconcel, S. N. S.; Baas, A. S.; Maynard, H. D. FDA-Approved Poly(Ethylene Glycol)-Protein Conjugate Drugs. Polymer Chemistry 2011, 2 (7), 1442–1448. https://doi.org/10.1039/c1py00034a.
We have demonstrated the synthesis pDNA bottlebrush polymers via modified polyethylene glycol monomethyl side chains. Agarose gel analysis allowed for easy characterization of the pDNA bottlebrush polymers. These results provide a facile route for a grafting-to approach for PEGylation of pUC19 plasmid DNA.
Future work includes getting AFM images of the plasmid-PEG conjugates and a restriction digest study to confirm chemical modification and overall structure.
Figure B. Reaction scheme for synthesis of mPEG-mesylate. All structures were confirmed using 1H NMR. n = 750, 2000, 20000
Figure C. Reaction scheme for synthesis of mPEG-diethanolamine. All structures were confirmed using 1H NMR. n = 750, 2000, 20000
lpUC19 plasmid
2686bp
Various molecular weight mPEG modified with mustargen end group
A
B
Figure F. 2.5% agarose gel showing increasing molar equivalence of mPEG-mustargen relative to pDNA (10-60 equivalence) A) mPEG2000 B) mPEG750
10 eq.
20 eq.
30 eq.
40 eq.
50 eq.
60 eq.
lpUC19
lpUC19
10 eq.
20 eq.
30 eq.
40 eq.
50 eq.
60 eq.
Owen Durant,1 Nicholas Pierini,2 Nate Oldenhuis2
2Department of Chemistry, University of New Hampshire, Durham, NH