## Slide 1: ASCE Concrete Canoe Cormac MacPhail, Lauren Robbins, Dustin Wells Department of Civil Engineering, University of New Hampshire, Durham, NH 03824
The ASCE Concrete Canoe competition is a nation-wide competition challenging students to build and race canoes made of concrete. The competition has been happening since the 1960’s and is well known by civil engineers across the country. Each year a new set of guidelines is provided to specify the mix-design and construction of the canoe. The goal of this project is to use engineering skills to create a proper concrete mix-design and to design and build a canoe that is hydrodynamic.
Innovation & Sustainability
Mix Design and Materials
Introduction
Acknowledgements
Hull Design
Construction Methods
COMMITTEE ON CONCRETE CANOE COMPETITIONS, and Jason Marshall. “2023American Society of Civil Engineers® Concrete Canoe Competition™ REQUEST FOR PROPOSALS.” Adobe Document Cloud for SharePoint/OneDrive, American Society of Civil Engineers, 6 Sept. 2022, https://documentcloud.adobe.com/spodintegration/index.html?locale=en-us.
“Standard Test Method for Compressive Strength of Cylindrical Concrete Specimens.” ASTM International - Standards Worldwide, 9 Mar. 2021, https://compass.astm.org/content-search/?content=c39&stype=A. C39-C1709
References
A Special Thanks to:
Dr. Dave, Noah MacAdam, Dr. Han
Our Sponsors: H&H, AECOM, Columbia, TFMoran, Emanuel, ASCE NH, Hoyle Tanner, John Ingwersen
All other supporters
Plywood ribs cut to inner cross section
Ribs connected with XPS foamboard
Foam mold sanded to shape
Concrete mix placed on the foam mold
Concrete cured and removed from the mold
Flotation endcaps placed, and walls sanded. Concrete stain to be applied on exterior
Concrete proportioning table.
2023 Rules for Mix Design and Construction
Maximum 30% Portland cement in cementitious materials mix
Maximum longitudinal hull dimension restricted to 22'
No paint, only dye or stain to color the concrete
Mesh reinforcement min. 40% open area
Floatation must be 3’ from endcaps and fully encased in concrete
All reinforcement must be fully encased in concrete
Only clear non-pigmented sealers may be applied adhering to ASTM C1315
Sustainability is a large part of the concrete canoe competition based on the carbon footprint from production of cementitious materials, efficient materials use, and other environmental impacts.
Poraver expanded glass is made of 100% recycled glass
Supplementary cementitious materials:
  Slag is a by-product of metal smelting
  Silica fume is a by-product of metal smelting
  Fly ash is a by-product of coal-powered plants
Eco stain containing zero volatile organic compounds to reduce chemical leaching into water
Chart: 
| 1E-4 | 9 | 17 | 28
Final Mix Compressive Strength | 1 | 1792 | 2748.25 | 2433.75
The compressive strength of the concrete after 28 days of curing is about 2500psi.
Two sizes of Poraver expanded glass were chosen to fit gradation requirements as shown above.
Photo of a broken sample under to microscope. Air bubbles can be seen in the aggregate.