## Slide 1: Predicting fracture toughness with microstructure sensitivity using an elasto-viscoplastic fast Fourier transform model
Authors: , , ,
,
4/15/2024

## Slide 2: Motivation
Experiments
FEM
Traditional methods of measuring and simulating fracture toughness are time consuming and inefficient
2
4/15/2024
Notes: Fracture toughness tests determine a material's resistance to crack propagation and therefore fracture, which is one of the fundamental material properties. To implement a fracture toughness test, you will first need to prepare a testing sample that has a pre-initiated crack. Preparation of samle for such test is time consuming, expensive and inefficient. Therefore, minimizing number of experiments and simulating fracture toughness test became a priority.
Most common technique for simulating fracture and cracking phenomena is FE method. Even thought, it has lots of advantages over experiments, FE analysis requires huge amount of time to prepare the model (clean the model, create the crack-cut , meshing) and requires significant computational resources in order to simulate fracture tougness test.
On the other side, Green’s function methods showed to be a good alternative to FE solvers of the field equations over spatial domains. These methods are attractive because the fast Fourier transform (FFT) algorithms can be used to solve the convolution integral representing equilibrium in stress under the strain compatibility over voxel-based microstructural cells yielding substantial computational efficiency. Moreover, the models are suitable to run in parallel, which makes this method a great competitor to FE methods, and I will show the analysis in the following slides.
Another maybe most important advantage of simulations is that by reusing the same model we can explore the impact of microstructure and grain orientation on toughness of the material, creating distributions of fracture toughness values, which is imposible to do experimentaly.

## Slide 3
Formulation
Green’s function for periodic b.c. is analytically available:
Periodic microstructure
Periodic b.c.
Standard FFT method
Non-periodic velocity boundary conditions
4/15/2024
Notes: Slides 3-5 EVPFFT method is based on Green’s function method. Green’s function is analytically available for simple boundary conditions like periodic or uniform applied strain in infinite medium. In case of complex arbitrary velocity b.c., Green’s function is not known analytically and is quite computationally expensive to find it. That is why instead of deriving Green’s function for specific applied b.c., different approaches are used. One such approach is method of images, where we still use the known analytical expressions for periodic or infinite Green’s function. The domain is extended, and additional sources are placed in the extended region, which enforce the desired b.c. in the original domain. Method was initially developed in electrostatics (example). We will use the same strategy, we will extend our domain, and apply a polarization field in the extended domain in order to enforce the boundary conditions in the original domain (Gelebart).

## Slide 4
Formulation
Green’s function for arbitrary non-periodic b.c. is not available:
1) Calculate Green’s function for each applied b.c. -> very computationally expensive
2) Apply b.c. using a different method.
Method of images:
Electrostatics Green’s function method
Boundary condition
Extend the domain, remove b.c. and introduce additional sources.
Non-periodic velocity boundary conditions
4/15/2024
Notes: One such approach is method of images, where we still use the known analytical expressions for periodic or infinite Green’s function. The domain is extended, and additional sources are placed in the extended region, which enforce the desired b.c. in the original domain. Method was initially developed in electrostatics (example). We will use the same strategy, we will extend our domain, and apply a polarization field in the extended domain in order to enforce the boundary conditions in the original domain (Gelebart).

## Slide 5
Formulation
Problem becomes periodic and Green’s function is available:
Method of images:
Extended domain with an eigenstress/strain field which enforces desired boundary conditions in the original domain.
Electrostatics Green’s function method
Boundary condition
Non-periodic velocity boundary conditions
M. Zecevic, R.A. Lebensohn: “Extension of FFT-based micromechanical formulations to consider general non-periodic displacement boundary conditions”, in preparation.

## Slide 6
Developed Python script for cutting crack mouth
Problems with features that consist of multiple separate geometries, that were staying as leftovers after cutting
Developed Sculpt script for meshing complex models
Softwares used: Cubit (sculpt)
  FE model preparation for fracture toughness simulations

4.5 M brick elements


measured microstructure
processed microstructure
cutted
mesh
4/15/2024
Notes: Pictures talk for itself.
I will spend next couple minutes explaining how this is done in FEs to reinforce my message how EVPFFT is more convenient. I have spent a lot more time getting results with FE method comparing to the EVPFFT code.

## Slide 7
Selected surface nodes
KlC velocity boundary conditions applied on the
process zone boundary- selected nodes
  Applying boundary conditions
K dominant zone
Process zone
4/15/2024
Notes: This is applied to create analytical results and numerical result using FE method and EVPFFT for verification

## Slide 8
[µm]
Analytical solution
[µm]
  Linear Elastic, Isotropic Crack-Tip Displacement field in X and Y direction for Mode I
Abaqus numerical solution
EVPFFT numerical solution
4/15/2024
Notes: Results are comparison between analytical solution- and two numerical-FEM and EVPFFT. The fields present displacement in X and Y direction. EVPFFT successfully validated.

## Slide 9
  Linear Elastic, Isotropic material von Mises Stress and Strain Field ahead of a crack Tip for Mode I
Elastic stored energy at the crack tip
Analytical solution
Abaqus numerical solution
EVPFFT numerical solution
14.12049 GPa
14.12092 GPa
14.07128 GPa
4/15/2024
Notes: Results are comparison between analytical solution- and two numerical-FEM and EVPFFT. The fields present VMS and Elastic Eeq. EVPFFT successfully validated.

## Slide 10
  Calibration of EVPFFT for plasticity
:
Material properties for stainless steel 304:
PF of initial texture
Anglin, B.S., Gockel, B.T. & Rollett, A.D. Developing constitutive model parameters via a multi-scale approach. Integr Mater Manuf Innov 5, 212–231 (2016).
https://doi.org/10.1186/s40192-016-0053-4
=109.500
=57.58
=855.375
=242.811
Notes: Calibration of EVPFFT for plastic simulation. Stress – strain curve matches experimental data. Rest talks for itself.

## Slide 11
  Plastic simulation-Von Mises Stress and Strain Field ahead of a crack Tip for Mode I
Crack tip radius: =0.00647
Crack length: =1.016617
=0.02093
max 1.031
max 281.021
max 1.031
11
4/15/2024
Notes: Reference model, which plastic stored energy is used for creating distributions of fracture toughness values. VMS and Eeq fields provided on the pictures. Upper pictures contain grain boundaries.

## Slide 12
Plastic stored energy:
where:
– stress on the grid at increment n [MPa]
– plastic strain rate on the grid at increment n [1/s]
– grid spacing in reference configuration [mm]
– deformation gradient
– time increment [s]
– volume of element in current configuration
– total plastic dissipation [mJ]
Plastic stored energy ↔ Fracture toughness
Back calculation of fracture toughness given the imposed displacement
corresponding to the prescribed value of the plastic stored energy:
Node coordinates and are converted from Cartesian to Polar and
, where and are displaced coordinates of the crack tip
4/15/2024
Notes: Core of the method for getting distributions explained with equations.
Reference model gave us plastic stored energy, that was a breaking point in the simulations for estimating fracture toughness and creating distributions.

## Slide 13
84 orientations
Normal distribution
μ= 119.096
σ = 1.96894
Distribution of Fracture toughness – crystal orientation
Fundamental zone
All grains touching crack tip have single orientation from fundamental zone
4/15/2024
Notes: Distribution number 1, that depends on crystal orientation through the crack. We set crack surrounding grains to have the same grain orientation (we get orientations from fundamental zone) and estimate Kic for each of the orientations from FZ. In this case, distribution was created using 84 orientations.

## Slide 14
10° rotation
Normal distribution
μ = 120.552
σ= 3.30972
Distribution of Fracture toughness – microstructure
45° rotation
Notes: Distribution number two that depends on microstructure. We are rotating the crystal orientations and the spatial coordinates of the grain structure for 10 degrees, creating a distribution of Kic with 36 simulations.

## Slide 15
Conclusions
*Methodology using EVPFFT developed for predicting fracture toughness with explicit consideration of microstructural variability
*We obtained a statistical distribution of fracture toughness as a function of local microstructures surrounding long cracks
*Experimentally distributions of fracture toughness are impossible to get !
4/15/2024
Notes: The methodology developed provides a practical simulation tool for predicting a distribution of fracture toughness with explicit consideration of microstructural variability.

## Slide 16
4/15/2024
Notes: Questions/thoughts?