## Slide 1: From Glycerol to Propanediols: Converting Biodiesel Byproducts to Feedstock Chemicals
Seth Drahusz
Department of Chemical and Bioengineering
University of New Hampshire
April 15th, 2024

## Slide 2
2
We need a more sustainable production of commercial products!

## Slide 3: Biodiesel is a Promising Alternative
3
Glycerol
Sustainable Energy Fuels, 2022, 6, 596–639

## Slide 4: Can We Valorize Glycerol?
Sustainable Energy Fuels, 2022, 6, 596–639
4

## Slide 5: Convert Glycerol to Feedstock Chemicals
5
1,2-propanediol (1,2-PDO)
1,3-propanediol (1,3-PDO)
Catalysis Today 291 (2017) 195–203
Sustainable Energy Fuels, 2022, 6, 596–639
Notes: Might need to change title

## Slide 6
Ir-Re
Pt-W
Activity
H2 Pressure
Metal Loading
6

## Slide 7
TiO2
1,3-PDO
Glycerol
7
Synergy
Support
Surface sites
Pt
HPA
H2
H+
H-

## Slide 8: Surface W Dictates 1,3-PDO Selectivity
AP: No pretreatment
C: Calcined @ 400°C for 4h in air
R: Reduced @ 300°C for 1h in H2
8

## Slide 9: Higher Reduction Temperature Favors PDO Formation
9

## Slide 10: Summary
Conversion of glycerol offers a sustainable pathway for chemical production
Pt-W based catalysts selectively convert glycerol to propanediols
Product distribution and activity varied with synthesis and pretreatment
10
Acknowledgements
Department of Chemical and Bioengineering | UNH Graduate School | Dr. Nan Yi