## Slide 1: Waste to Wealth: Carbon Dioxide Conversion to Fuels Jaxon Boudreau, Dr. Nan Yi Chemical Engineering and Bioengineering, University of New Hampshire, Durham, NH 03824
Global warming impacts the health of ecosystems around the world [1]
Efficient and effective removal of greenhouse gas emissions mitigates environmental impact
Catalysis plays a critical role in the chemical conversion of carbon dioxide
Catalysts have the ability to adjust the rate of a chemical reaction
The goals of catalytic design are to produce a selective, active, and stable material
Nickel –Titanium Dioxide – Heteropoly Acid Catalysts
Broad Impact
Acknowledgements
Nickel-Silver / Copper-Silver Supported Catalysts
Bulletin of the American Meteorological Society, 2005, 86, 1571
Chemical Society Reviews, 2014, 43, 8226
Resources Policy, 2015, 45, 255
References
Catalysis
Dr. Nan Yi’s research group at the University of New Hampshire (special thanks to Matthew Noyer)
Dr. John Monnier’s research group at the University of South Carolina
Hamel Center of Undergraduate Research
The National Science Foundation
Figure 1. Effect of a catalyst on a chemical reaction [2]
Metal | Price Per Ounce
Copper (Cu) | $0.21
Nickel (Ni) | $0.66
Silver (Ag) | $19
Platinum (Pt) | $881
Gold (Au) | $1,715
Palladium (Pd) | $1,945
Rhodium (Rh) | $15,350
- Base metal (Cu or Ni)
Galvanic displacement
Reduction Potential
Thermal Gravimetric Analysis
Table 1. Cost of precious metals [3]
Summary
Galvanic displacement is a well-controlled kinetic process
Amount of base metal that can be galvanically displaced is determined by i) temperature and concentration of reducible cation; ii) fraction of base metal existing in zero-valent state
Reaction time becomes an important variable for lower rates of displacement
- Support (SiO2 or Al2O3)
Chart: 10Ni[15H3PA/TiO2]
Summary
Optimal calcination temperature is 300oC
The addition of heteropoly acid affects the interaction between nickel and titanium dioxide
Lower heteropoly acid loading leads to higher carbon dioxide conversion
Chart: Temperature (ºC)
| 250 | 300 | 325 | 350 | 375 | 400 | 450
10Ni[5HPA/TiO2] | 4.3985 | 7.0034 | 11.188 | 9.1708 | 14.7402 | 29.0959 | 49.172
10Ni[15HPA/TiO2] | 1.113 | 1.7499 | 5.1275
10Ni[10HPA/TiO2] | 3.2469 | 4.5543 | 11.2295
10Ni[3HPA/TiO2] | 6.9879 | 14.9107 | 58.6586
10Ni[5H3PA/TiO2]
10Ni[15H3PA/TiO2]
10Ni[10H3PA/TiO2]
10Ni[3H3PA/TiO2]
Chart: Time (Min)
| 0 | 2 | 5 | 10 | 30 | 60 | 180 | 240
Ag⁺, 25℃ | 0.45631 | 0.33107 | 0.31141 | 0.30649 | 0.2925 | 0.25918 | 0.21329 | 0.20225
Ag⁺, 50℃ | 0.43799 | 0.24822 | 0.2023 | 0.18634 | 0.1689 | 0.15199 | 0.13903 | 0.13339 | 0.12624 | 0.12407
Ag⁺, 70℃ | 0.23768 | 0.18614 | 0.1748 | 0.15711 | 0.14562 | 0.12568 | 0.10499 | 0.078429
Chart: Time (Min)
| 0 | 2 | 5 | 10 | 30 | 60 | 180 | 240
Cu²⁺, 25℃ | 0.0053111 | 0.059343 | 0.066896 | 0.07157 | 0.080823 | 0.096119 | 0.1201 | 0.12496
Cu²⁺, 50℃ | 0.0045794 | 0.093145 | 0.11524 | 0.12175 | 0.14045 | 0.15126 | 0.15749 | 0.17085 | 0.18525 | 0.19011
Cu²⁺, 70℃ | 0.12884 | 0.11939 | 0.12265 | 0.12232 | 0.14087 | 0.15796 | 0.20668
Future Work
Hydrogen Temperature Programmed Reduction
Pretreatment: 450oC for 2 hours with 30%H2/He
Reaction Conditions: CO2/H2/He 1:4:18 |
0.1g | 52.5 mL/min
Chemisorption to determine the active sites
Scanning Transmission Electron Microscopy analysis to understand the morphology
Chart: Time (Min)
| 0 | 1 | 3 | 5 | 10 | 30 | 60 | 120 | 180
Ag⁺, 25℃ | 0.47315 | 0.45086 | 0.44972 | 0.44535 | 0.42955 | 0.43061 | 0.40438 | 0.39131 | 0.36942
Ag⁺, 50℃ | 0.47639 | 0.39482 | 0.37629 | 0.3467 | 0.32623 | 0.32623 | 0.34245
Ag⁺, 70℃ | 0.46429 | 0.37449 | 0.3269 | 0.28618 | 0.28084 | 0.26602 | 0.26652 | 0.29747
Chart: Time (Min)
| 0 | 3 | 5 | 10 | 30 | 60 | 120 | 180
Ni²⁺, 25℃ | 2.5557e-05 | 0.0044468 | 0.0039357 | 0.0087914 | 0.014874 | 0.026323 | 0.038028 | 0.043497
Ni²⁺, 50℃ | -0.0052902 | 0.0046513 | 0.027243 | 0.034604 | 0.050244 | 0.071609 | 0.073603 | 0.073245
Ni²⁺, 70℃ | -0.0055458 | 0.027192 | 0.043855 | 0.052084 | 0.066089 | 0.082394 | 0.085103
Titanium Dioxide
(TiO2)
Heteropoly Acid
(H3PW12O40 | H3PA)
Activity Test