## Slide 1
Photocatalytic Methane Conversion over Heteropoly Acid Based Catalysts
Jack Sullivan and Dr. Nan Yi
Department of Chemical Engineering and Bioengineering, University of New Hampshire, Durham, NH 03824
Acknowledgments
Summary
References
Methane (CH4) is an abundant greenhouse gas
Ethane (C2H6) and Hydrogen are higher value fuels
Photocatalysis can overcome large energy inputs associated with thermal conversion
Photocatalytic methane conversion makes sustainable methane transformation feasible
The synergy between heteropoly acid and gold enables the production of ethane and hydrogen at moderate conditions
Brookite phase TiO2 may facilitate methane conversion
[1] Overview of Greenhouse Gases. EPA, 2024
[2] Nat. Rev. Mater. 2022, 7 (8), 617–632.
[3] Nat. Energy 2020, 5 (7), 511–519.
Gold facilitates C-H bond cleavage
Heteropoly Acid (HPA) promotes photocatalytic performance
Photocatalytic activity testing
CH4 (10%)
He (90%)
Au- HPA-TiO2
CH4
C2H6 CO2
h
Advantages of a Flow Reactor:
Allows for continuous methane conversion
Mitigate overoxidation through decreased contact time
Non-Oxidative Methane-Ethane Conversion
UNH Hamel Center for Undergraduate Research, Seth Drahusz, and Darcy Silver
Activity Optimization of Au-HPA-TiO2 Catalyst
Introduction
(0.5)Au-TiO2
Regeneration 2
Regeneration 1
Catalyst Synthesis
Activity Testing
US Methane Emissions
Regeneration 2
Regeneration 1
(0.5)Au-(10)HPA-TiO2
Sol-Gel
Anatase
P25
Sol-Gel TiO2 Exhibits Superior Ethane Production
Ethane Yield vs. TiO2 Supports
Light Off
Light Off
Lamp ON | OFF
Effect of Calcination Temperature
0.25 wt. %
0.5 wt. %
1 wt. %
Effect of Gold Loadings
Amount (area/gcat)
(0.5)Au-HPA-TiO2
(0.5)Au-TiO2
Role of HPA
HPA Increases Ethane Selectivity
Endo Exo
How Does HPA and TiO2 Effect Activity?
TiO2
Au-HPA-TiO2
HPA-TiO2
Raman Spectra of Au-HPA-TiO2, HPA-TiO2, and TiO2
Sol-Gel TiO2 Contains Anatase and Rutile Phases
Regenerative Studies
Thermogravimetric Analysis of (5)Au-HPA-TiO2
(0.5)Au-HPA-TiO2
Light ON/OFF Test
Initial
Initial
Gold Loading | Calcination Temperatures | TiO2 Support
Wet Impregnation Method of Au-HPA-TiO2
HAuCl4
2
Room Temperature
Visible
UV
Heteropoly Acid
Gold