## Slide 1
Results and Discussion
Introduction
Future Work
This research is funded by National Science Foundation EPSCoR award #1757371, NH BioMade.
Thanks to Yung Chun Lin for his work with the SEM particle experiments.
Photoinduced Cycloaddition Dimerization for Directed-Assembly of Microparticles Anna Huebner1, John Tsavalas1,2
(1) Department of Chemistry and (2) Materials Science Program, University of New Hampshire, Durham, NH
Project Goal
Nuclear Magnetic Resonance Spectroscopy
References
Acknowledgements
Scanning Electron Microscopy
UV-Visible Spectroscopy
Methods
Chart: YL 3-28 no irradiation
The photodimerization of anthracene is one of the oldest documented photochemical reactions and has been widely studied and used in a variety of applications, such as making gates on caged host complexes, as it provides a reversible reaction that can occur hundreds of times without creating side products1,2 Undergoing a [4+4] cycloaddition when exposed to light at wavelengths above 300 nm, the dimerization can be reversed under the application of heat or wavelengths of light under 300 nm illustrated below.3
We want to investigate the application of the anthracene photodimerization reaction for creating a trigger to lock microparticles into an ordered assembly. The further application of this research is to extrude multi-lobed particles containing anthracene in each lobe through a 3D printer to form a scaffolding for tissue engineering, and then lock the assembled particles in place with UV light by leveraging the anthracene dimerization between neighboring particles.
After UV irradiation
Before UV irradiation
Anthracene was incorporated into polymer particles via emulsion polymerization. Techniques to assess dimerization include:
UV-visible spectroscopy (UV-vis)
Nuclear magnetic resonance spectroscopy (NMR)
Scanning electron microscopy (SEM).
Experiment with a variety of particles and conditions to determine if there is a set of conditions that allows for dimerization between anthracenes on neighboring particles
Synthesize a longer pendant anthracene and incorporate that into the surface of the particles for dimerization.
Conclusions
UV-vis and NMR show the anthracene on the surface of the particles are dimerizing
SEM shows the dimerization may be between anthracene on the same particle, rather than between neighboring particles
[1] Wang, H.; Liu, F.; Helgeson, R. C.; Houk, K. N. Reversible Photochemically Gated Transformation of a Hemicarcerand to a Carcerand. Angew. Chemie – Int. Ed. 2013, 52 (2), 655–659. https://doi.org/10.1002/anie.201205376.
[2] Xu, J. F.; Chen, Y. Z.; Wu, L. Z.; Tung, C. H.; Yang, Q. Z. Dynamic Covalent Bond Based on Reversible Photo [4 + 4] Cycloaddition of Anthracene for Construction of Double-Dynamic Polymers. Org. Lett. 2013, 15 (24), 6148–6151. https://doi.org/10.1021/ol403015s.
[3]Breton, G. W.; Vang, X. Photodimerization of Anthracene. A [4p+4p] Photochemical Cycloadddition J. Chem. Educ. 1998, 75 (1), 81–82.
Chart: YL 3-28 Photodimerization
Our group is currently working on a project to use rationally designed polymer particles to create a hierarchically structured porous material that can be
printed through a 3D printer to form a tissue engineering scaffolding. To print through the syringe of the 3D printer the material must be a viscous liquid. Once it is printed, there needs to be a trigger to lock the particles into place to
Dimerization of anthracene is evidenced in UV-vis by:
Characteristic peaks at 255, 345, 365, and 385 nm
Decrease in absorption as irradiation time increases
Particle size | Seed | Second stage
500 nm | PMMA | -HMA -MMA -9-anthracenyl methyl methacrylate
Particle size | Seed | Second stage
370 nm | MMA | -MMA -9-anthracenyl methyl methacrylate (10 wt %)
Seed | Second stage
PMMA | -HMA -MMA -9-anthracenyl methyl methacrylate
Left: Original particles. Right: Particles that were irradiated and mixed with THF.
UV-vis of irradiated particles
UV-vis of particles with no irradiation
form a solid scaffolding for tissue to grow on. Inspired by the UV irradiation capability of our 3D printer and the widely used photodimerization of anthracene, we began investigating the use of the anthracene dimerization reaction to lock these particles into place.