## Slide 1
High-performance full-field crystal plasticity with dislocation-based hardening and slip system back-stress laws: Application to modeling deformation of dual-phase steels
Adnan Eghtesad
[Department of Mechanical Engineering, University of New Hampshire, Durham, NH 03824, USA]
Kai Germaschewski
[Department of Physics, University of New Hampshire, Durham, NH 03824, USA]
Ricardo A. Lebensohn
[Materials Science and Technology Division, Los Alamos National Laboratory, Los Alamos, NM 87544, USA]
*Marko Knezevic
[Department of Mechanical Engineering, University of New Hampshire, Durham, NH 03824, USA]

## Slide 2
Computational Crystal Plasticity
Marko Knezevic
Milan Ardeljan
William Feather
Dan savage
Milovan Zecevic
Timothy J. Barrett
Zhangxi Feng
Sowmya Daroju
Adnan Eghtesad
Marko Knezevic
Miroslav Zecevic
Evgenii Vasilev
Eftekhar Riyad
Adnan Eghtesad
Adnan Eghtesad

## Slide 3
EVPFFT (Elasto-Visco-Plastic Fast Fourier Transform ) micromechanical full-field solver
Grid
Voxels
Solid RVE
[111]
[101]
[001]
Voxels
(FFT sampling points)
Discretized RVE
Texture evolution, monotonic
and cyclic deformation
Qualification and quantification
of micromechanical fields
(a) DP590
(b) DP980
(c) DP1180
(d) MS1700

## Slide 4: Mathematics behind EVPFFT
Constitutive Equations for CP framework
…
Green’s solution for
displacement field
Physics-based dislocation density hardening law
Texture update

## Slide 5
Motivation behind high-performance
computing development of EVPFFT

## Slide 6
Simulating such high-resolution microstructure (~17 million FFT points) will take months of run …
However, such resolution is necessary to capture the field gradients at GB, more accurately.
DP 590 steel microstructure
High-res fields
# of voxels:

## Slide 7
Parallel EVPFFT
MPI
GPU
Multi-GPU
OpenMP
Hybrid OpenMP MPI
EVPFFT Parallel versions
Parallel FFTs
MPI FFTW
CUFFT
Threaded FFTW
Parallel FFTs running within EVPFFT
High-performance EVPFFT on distributed hybrid GPU-CPU architecture

## Slide 8
NVIDIA TESLA V100, the current world leading GPU computing architecture [GPU-EVPFFT : up to 43x speedup on single GPU, expected speed up on 10 GPUs: 430X, yet to be tested on BioMade supercomputer]
UNH RCC : Trillian Cray, BioMade, Mech 3-9 servers
Perfect strong scalability on Multiple GPUs tested on Titan @ Oak ridge national lab running on 128 K20X GPUs

## Slide 9: Simulation of Martensitic-Ferritic dual phase steels under monotonic and cyclic loading

## Slide 10
DREAM3D microstructure based on the SEM images of Ferritic-Martensitic phase distributions for
DP590, DP980, DP1180, and MS1700
Measured textures
(MS1700 is almost uniform)
(a) DP 590 (7.7% martensite)
(b) DP 980 (39% martensite) (c) DP 1180 (45% martensite)
(d) MS 1700 (80% martensite)

## Slide 11: Prediction of elastic anisotropy based on crystal mechanics
Elastic response:

## Slide 12
Comparison of measured and calculated variation of effective Young’s modulus and Poisson’s ratio as a function of in-plane sheet orientation. The angle starts from the rolling direction (i.e. 0° = RD).
Contour plots showing anisotropy of Young’s modulus with orientation for single crystalline

## Slide 13
Elasto-Plastic response:
Calibration of monotonic loading

## Slide 14
Calibration of monotonic response using single set of DD hardening parameters for all steel variants
Dislocation density hardening parameters for Ferritic and Martensitic phases

## Slide 15
Calibration of cyclic loading:
i. Reversibility and dislocation annihilation
ii. Slip-system-level Kinematic Back-stress hardening
and Bauschinger effect

## Slide 16: Dislocation annihilation (reversible DD) in EVPFFT
Reversible DD hardening
(c)
Dislocation annihilation
Dislocation annihilation

## Slide 17: *No BS
Back-stress can help here to account for Bauschinger effect

## Slide 18
A slip-system-level kinematic piece-wise back-stress phenomenological hardening law in EVPFFT that saturates exponentially and mimics the Bauschinger effect
Back-stress can either help or hinder resolved shear stress on a slip plane
Back-stress hardening law

## Slide 19
Back-stress hardening parameters for Ferritic and Martensitic phases

## Slide 20
Qualification of Micromechanical fields
(An advantage of EVPFFT as full-field crystal plasticity solver over EPSC [Elasto-plastic self consistent] )

## Slide 22
Quantification of field gradient across the inter-granular grain boundaries

## Slide 24: Future work
Incorporate the multi-GPU EVPFFT solver to Finite Element
(Accelerated UMAT for ABAQUS). Run the FEM on MPI while
the underlying Microstructure RVE on GPU. This is to facilitate
arbitrary BCs and geometries